MINERAL RESOURCES TASMANIA

Laboratory Report

LJN2021-039

# Sand Size ANALYSES,

# Lake River Quarry

MINERAL RESOURCES TASMANIA

Laboratory Report

LJN2021-039

# Sand Size ANALYSES,

# Lake River Quarry

An unpublished Mineral Resources Report for:

Jessica Renaud

An unpublished Mineral Resources Report for:

Jessica Renaud

By: 	R S Bottrill,

L Unwin and Ross King

Date:	23 April 2021

By: 	R S Bottrill,

L Unwin and Ross King

Date:	23 April 2021

Mineral Resources Tasmania

Department of State Growth

Mineral Resources Tasmania

Department of State Growth

# Summary

The results indicate that both samples are mostly gravel (68 & 87wt.%) with some sand and negligible clay or silt fractions. The Uniformity Coefficients are 14 and 2 and the Effective Sizes are is 500 and 1300 microns.

# Introduction

Two samples of a soil and rock mix were submitted for sizing analysis by Jessica Renaud, MRT. The sample details are shown in Table 1.

Table 1: Sample details

| Reg. # | Location | Sample Description |
| --- | --- | --- |
| C113488 | Lake River Quarry Upper | Soil and Rock mix |
| C113489 | Lake River Quarry Lower | Soil and Rock mix |

# METHODS

The samples were dried for 48 hours at 50 degrees C and then machine sieved for 15 minutes.

Sample descriptionS

The samples are both poorly sorted mixtures of weathered rock, mostly medium to coarse gravel but including clay, silt and sand, up to about 50mm in size, with a medium red-brown colour.

SIZING

The samples were machine sieved, using Australian standard sieves. Each fraction was weighed and determined as a proportion of the total sample.  The results are shown in Tables 2 - 5 and Figures 1 & 2.

Table 2: Size analysis summary (Wt.%) – C113488

|  | Size range (microns) | wt.% |
| --- | --- | --- |
| gravel | >2000 | 67.95 |
| very coarse sand | 1000-2000 | 13.19 |
| coarse sand | 500-1000 | 8.94 |
| medium sand | 250-500 | 5.29 |
| fine sand | 125-250 | 2.58 |
| very fine sand | 63-125 | 1.26 |
| silt | 2-63 | 0.79 |
| clay | <2 | 0.00 |
| Total |  | 100.00 |

Fig.1. Cumulative size analysis C113488

Table 3: Size analysis summary C113488

| d60 | Size for 60% passing (microns) | 6800 |
| --- | --- | --- |
| d10 | Size for 10% passing (microns) | 500 |
| UC | UC = uniformity coefficient = d60/d10 (ie. 60% passing/10% passing) | 14 |
| ES | ES = Effective Size = d10 (ie. 10% of media passing) | 500 |

Table 4: Size analysis summary (Wt.%) – C113489

|  | Size range (microns) | wt.% |
| --- | --- | --- |
| gravel | >2000 | 86.96 |
| very coarse sand | 1000-2000 | 4.60 |
| coarse sand | 500-1000 | 3.46 |
| medium sand | 250-500 | 2.45 |
| fine sand | 125-250 | 1.41 |
| very fine sand | 63-125 | 0.81 |
| silt | 2-63 | 0.32 |
| clay | <2 | 0.00 |
| Total |  | 100.00 |

Fig.2. Cumulative size analysis C113489

Table 5: Size analysis summary C113489

| d60 | Size for 60% passing (microns) | 2910 |
| --- | --- | --- |
| d10 | Size for 10% passing (microns) | 1300 |
| UC | UC = uniformity coefficient = d60/d10 (ie. 60% passing/10% passing) | 2 |
| ES | ES = Effective Size = d10 (ie. 10% of media passing) | 1300 |

Conclusions and Discussion

The results indicate that C113488 is mostly gravel (68wt.%) with some sand and negligible clay or silt fractions. The Uniformity Coefficient is 14 a and the Effective Size is 500 microns.

The results indicate that C113489 is mostly gravel (87wt.%) with some sand and negligible clay or silt fractions. The Uniformity Coefficients is 2 and the Effective Size is 1300 microns.

# R.S. Bottrill 					L Unwin

# Mineralogist/Petrologist 	TECHNICAL OFFICER

# Disclaimers:

While every care has been taken in the preparation of this report, no warranty is given as to the correctness of the information and no liability is accepted for any statement or opinion or for any error or omission. No reader should act or fail to act on the basis of any material contained herein. Readers should consult professional advisers. As a result the Crown in Right of the State of Tasmania and its employees, contractors and agents expressly disclaim all and any liability (including all liability from or attributable to any negligent or wrongful act or omission) to any persons whatsoever in respect of anything done or omitted to be done by any such person in reliance whether in whole or in part upon any of the material in this report. The MRT laboratories are not NATA registered but work to similar standards. This and other data collected in MRT laboratories may enter the MRT databases but every attempt will be made to ensure it remains closed file and not be available externally, unless at your request.

Appendix 1: Sizing results

| Sample | C113488 |  |  |  |
| --- | --- | --- | --- | --- |
| Size range (microns) | wt. (g) | wt.% | cum.wt% passing | Sieve size (microns) |
| >50000 | 0 | 0 | 100 | 50000 |
| 25000-50000 | 376.74 | 15.25 | 84.75 | 25000 |
| 16000-25000 | 76.9 | 3.11 | 81.63 | 16000 |
| 8000-16000 | 443.13 | 17.94 | 63.69 | 8000 |
| 4000-8000 | 395.58 | 16.02 | 47.68 | 4000 |
| 2000-4000 | 385.90 | 15.62 | 32.05 | 2000 |
| 1400-2000 | 176.70 | 7.15 | 24.90 | 1400 |
| 1000-1400 | 149.13 | 6.04 | 18.86 | 1000 |
| 850-1000 | 61.78 | 2.50 | 16.36 | 850 |
| 710-850 | 59.12 | 2.39 | 13.97 | 710 |
| 600-710 | 53.71 | 2.17 | 11.79 | 600 |
| 500-600 | 46.10 | 1.87 | 9.93 | 500 |
| 355-500 | 71.66 | 2.90 | 7.03 | 355 |
| 250-355 | 59.00 | 2.39 | 4.64 | 250 |
| 180-250 | 35.50 | 1.44 | 3.20 | 180 |
| 125-180 | 28.31 | 1.15 | 2.05 | 125 |
| 106-125 | 9.15 | 0.37 | 1.68 | 106 |
| 90-106 | 9.14 | 0.37 | 1.31 | 90 |
| 63-90 | 12.95 | 0.52 | 0.79 | 63 |
| 50-63 | 14.17 | 0.57 | 0.21 | 50 |
| 38-50 | 5.30 | 0.21 | 0.00 | 38 |
| <38 |  | 0.00 | 0.00 | <38 |
| tot | 2469.97 | 100.00 |  |  |

| Sample | C113489 |  |  |  |
| --- | --- | --- | --- | --- |
| Size range (microns) | wt. (g) | wt.% | cum.wt% passing | Sieve size (microns) |
| >50000 | 0 | 0 | 100 | 50000 |
| 25000-50000 | 1340.82 | 47.31 | 52.69 | 25000 |
| 16000-25000 | 216.67 | 7.65 | 45.04 | 16000 |
| 8000-16000 | 484.53 | 17.10 | 27.95 | 8000 |
| 4000-8000 | 242.49 | 8.56 | 19.39 | 4000 |
| 2000-4000 | 179.89 | 6.35 | 13.04 | 2000 |
| 1400-2000 | 70.82 | 2.50 | 10.55 | 1400 |
| 1000-1400 | 59.63 | 2.10 | 8.44 | 1000 |
| 850-1000 | 25.18 | 0.89 | 7.55 | 850 |
| 710-850 | 26.22 | 0.93 | 6.63 | 710 |
| 600-710 | 24.39 | 0.86 | 5.77 | 600 |
| 500-600 | 22.25 | 0.79 | 4.98 | 500 |
| 355-500 | 35.98 | 1.27 | 3.71 | 355 |
| 250-355 | 33.43 | 1.18 | 2.53 | 250 |
| 180-250 | 21.59 | 0.76 | 1.77 | 180 |
| 125-180 | 18.35 | 0.65 | 1.12 | 125 |
| 106-125 | 6.58 | 0.23 | 0.89 | 106 |
| 90-106 | 6.45 | 0.23 | 0.66 | 90 |
| 63-90 | 9.86 | 0.35 | 0.32 | 63 |
| 50-63 | 4.99 | 0.18 | 0.14 | 50 |
| 38-50 | 3.97 | 0.14 | 0.00 | 38 |
| <38 |  | 0.00 | 0.00 | <38 |
| tot | 2834.09 | 100.00 | 213.19 |  |