## Slide 1: Thomas Creek Some “off the cuff” comments relating to recent drill assays
Compiled on behalf of AX8
By Dr N W Brand
28/08/2018
DISCLAIMER: The conclusions and recommendations expressed in this material represent the opinions of the author based on observations made and the available data. The opinions and recommendations provided from this presentation are in response to a request from the client and no liability is accepted for commercial decisions or actions resulting from them.
DISCLOSURE : The author holds no shares directly or indirectly in AX8

## Slide 2: Summary of Holes
TCDD002: most distal
  least altered, VMS signature, “dirty” pyrite (ie full of chalcophile elements) and chlorite dominant
TCDD001: outboard of the main mineralisation
  Altered with “dirty” pyrite, carbonate dominant yet with kick in sulphur at base
TCD003: mineralised
  Most altered, mica dominant and clean pyrite

## Slide 3: Some observations and comments
The dominant lithology is andesitic with monzodiorite present in TCDD001 and TCDD003 and mafics present in top 40 m of TCD002.
The monzodiorite is the MOST altered lithology and appears to have an influence on mineralisation.
  IE TCDD001 Co-Fe-S mineralisation lies directly above the monzodiorite
  IE TCDD003 Co-Fe-S mineralisation lies directly below the monzodiorite
The IP anomaly is explained by the presence of pyrite.
Pyrite controls cobalt and Co grade increasing pyrite concentration.
In holes TCDD001 & TCDD002 Cobalt-Pyrite (S-Fe-Co) is associated with a large suite of chalcophile elements including Cu, Mo, Bi, Mo, Te, Ag, Au, Ce, Pb, Re, Se, Sb, Cd, Ni in holes TCDD001 & TCDD002.
Mineralization upper contact in TCDD002 is marked by marked by a “VMS” signature including Pb, Zn, Ag & Cd
In TCDD003 Cobalt-Pyrite (S-Fe-Co) is separated from elevated Cu
TCDD001 is more altered than TCDD003 with TCDD002 the least altered
Mineralogy has an influence on sulphide mineralisation with carbonate having low sulphide content and mica (ie alerted) having high sulphur content (eg TCDD003)
At the base of TCDD001, sulphur content starts to increase (along with Ni) and may be a future target.
The sulphur content in TCDD003 increases with increasing depth

## Slide 4: Comment on Sulphides and IP anomaly

## Slide 5: Drill hole locations (ASX 20/08/2018)

## Slide 6: Sulphides – dominantly pyrite
Pyrite tie line
Pyrite is the dominant sulphide and in part explains the IP anomaly at Thomas Creek

## Slide 7: Sulphide control on Co
>400 ppm
>100 ppm
Cobalt is associated with the sulphides (pyrite) and Co grade increases with increasing sulphide concertation
Over range Sulphur
>200 ppm

## Slide 8: S vs Cu (coloured by Co)
Copper is also associated with pyrite with a number of sample align with chalcopyrite tie line
chalcopyrite tie line
pyrite

## Slide 9: Comments on TCDD001

## Slide 10: TCDD001
Discrete tight cluster of points representing a monzodiorite (as logged) with the main lithological package andesitic
The monzodiorite is the most altered lithology in hole TCDD001

## Slide 11: TCDD001
Co-Fe-S mineralisation lies directly above monzodiorite
Increasing Sulphur

## Slide 12: Associated elements
Co –S-Fe associated with a large suite of chalcophile elements including Cu, Mo, Bi, Mo, Te, Ag, Au, Ce, Pb, Re, Se, Sb, Cd, La, Ni

## Slide 13: Comments on TCDD002

## Slide 14: TCDD002
Lose cluster of points representing the main lithological package of andesitic with mafics
TCDD002 shows little alteration

## Slide 15: TCDD002
Broad zone of Co-Fe-S mineralisation within least altered rocks - ? Pyrite halo
anomalous Cu ? structural

## Slide 16: TCDD002 - Associated elements
Co –S-Fe associated with a large suite of chalcophile elements including Cu, Mo, Bi, Mo, Te, Ag, Ce, Pb, Re, Se, Sb, Cd, La, Ni, Zn

## Slide 17: TCDD002 - Base-metal Signature
NOTE upper contact of mineralised zone marked by a “VMS” signature including Pb, Zn, Ag & Cd

## Slide 18: Comments on TCDD003

## Slide 19: TCDD003
Lose cluster of points representing the main lithological package of andesitic along with a monzodiorite
The monzodiorite is the most altered lithology in hole TCDD003 The elevated Cu is logged as micromonzodiorite porphyry. dss cpy 0.25%.”

## Slide 20: TCDD003
Significant broad zone of Co-Fe-S mineralisation
anomalous Cu associated with logged micromonzodiorite
Co 5710 ppm
Increasing in S
NOTE elevated Co separated from elevated Cu

## Slide 21: TCDD003 - Associated elements
Co –S-Fe not associated with plethora of chalcophyle elements
Co 5710 ppm
Cu-Ag association
Significant broad zone of Co-Fe-S mineralisation
NOTE elevated Co separated from elevated Cu

## Slide 22: SWIR (ASD)
NOTE. The SWIR data presented here in is very basic.
No in-depth interpretation has been undertaken on the SWIR data to date such as extraction of key features to indicate temperature vector, degree of crystallinity, etc.

## Slide 23: TCDD001 - SWIR
Carbonate dominant
chlorite dominant
mica dominant
Chlorite Carbonate

## Slide 24: TCDD002 - SWIR
chlorite dominant
mica dominant

## Slide 25: TCDD003 - SWIR
Co 5710 ppm
Carbonate dominant
Carbonate-chlorite dominant
chlorite –mica dominant
mica dominant

## Slide 26: S vs Fe (SWIR minerals)
Mineralogy has influence on sulphide mineralisation with carbonate having low sulphide content and mica (ie alerted) having high sulphur content

## Slide 27: end